Jurnal Neutrino:Jurnal Fisika dan Aplikasinya, Vol. , No.
 [1]
Jurnal Neutrino Vol. 7,  No. 2 April 2015

    2
Jurnal Neutrino:Jurnal Fisika dan Aplikasinya, Vol. , No.
[3]

CHARACTERISTIC I-V OF Cu/Cu2O SOLAR CELLS WITH BELIMBING WULUH (AVERRO BILIMBI) ELECTROLYTE USING SUN SIMULATOR
Teuku Andi Fadlly1*, Fajriani1, Tisna Harmawan2 

1Department of Physics, Faculty of Enggenering, Samudra University
Jl. Meurandeh Langsa 24416
2Department of Chemistry, Faculty of Enggenering, Samudra University
Jl. Meurandeh Langsa 24416
ABSTRACT 
Characteristic I-V of Cu/Cu2O solar cells with belimbing wuluh electrolyte have been determind using sun simulator data by varying the resistor value (R). Resistor of 1-10 kΩ were applied. The Cu2O layer as a p-type semiconductor is formed by thermal oxidation plate Cu at a temperature of 550 °C. The thermal oxidation time is 80, 100, 120 minutes. Sun simulator measurement result showed that the eddition of thermal oxidation time improved the current (I) values, where the most improvement occured in Cu/Cu2O-100. Furthermore, the current dropped with increasing voltage (V) indicating increase the resistor value. Optimal power (Pout) increases with increasing applied time the thermal oxidation of Cu plate at 100 minutes. Plotting characteristic I-V give the efficiency (η) of solar cells from samples, and it was found that the highest value was reached by the Cu/Cu2O-100, ie. 0,28 %. In general, the more layers of Cu2O are formed, the higher the efficiency of solar cells.
Keywords: characteristic I-V; Cu/Cu2O; belimbing wuluh electrolyte; sun simulator; efficiency solar cells.

Introduction
Indonesia is one of the countries with a tropical climate which is located on the equator, so that the intensity of sunlight is quite large by the surface of the earth, especially in Aceh. Solar radiation energy is 4,5-5,1 kWh/m²/day(1). 
Kupro oxide or Cu2O is p-type semiconductor having an energy band gap 2 eV with high absorption coefficient and good carrier mobility(2). This is an alternative material that attracts attention to solar cell devices, in addition it is environmentally friendly, non-toxic, and easy to process in production(3). Non-vacuum techniques can be applied to produce Cu2O, such as electrochemical deposition (ECD) and thermal oxidation from Cu sheets(2). Cu/Cu2O solar cells have been investigated with an electrolyte, such as sea water media(1) and NaCl+water(4). The belimbing wuluh electrolyte in Cu/Cu2O solar cells, however, have not been studied particularly in terms of characteristic I-V.
This article reports the characteristic I-V Cu/Cu2O solar cells with belimbing wuluh electroly. Characteristic I-V data was used to determine the efficiency of solar cells. Study of the characteristic I-V of the Cu/Cu2O solar cells with belimbing wuluh electrolyte will expand their analysis prospects.
Methods 
The experiments used commercial Cu sheets. The Cu2O layer sampels were prepared using a thermal oxidation method from Cu sheets. Solar cell samples were prepared with dimensions 5 mm × 5 mm and 1 mm thickness which is compatible with the dimension for sun simulstor testing. The termal oxidation was carried out at a temperature of 550 °C(5) with a variation of the heating time (for 80, 100, 120 minutes). Solar cell electrolytes using belimbing wuluh extrack were obtained in Langsa city, Aceh. Belimbing wuluh was squeezed to take the liquid, then filtered. Cu2O layer plate is placed on a Cu plate with a distance of 10 mm, then placed in a glass container containing electrolytes from belimbing wuluh extract. 
Sun simulator is prepared with dimensions 100 mm × 100 mm and 150 mm height. In addition, the top side is given a hologen bulb lamp as a light source. The sun simulator is used for the characteristics I-V of solar cell connected to electronic circuits(6). The results were analyzed to obtain the fill factor (FF) and efficiency (η) of solar cell using the equation(7):
[image: image2.png]FF = ‘mak¥mak — Pour
LoV,




                              (1)

[image: image4.png]= Zoe = Tocke x 1009





        (2)

where, Voc is open-circuit voltage, Isc is short-circuit current, Pin is the total input power of light radiation cell/module, dan Pout is the optimal electrical power output cell/module.

Result and Discussion
Figure 1 shows a sun simulator using hologen lamps. The resulting spectrum of light bulb hologen lamp approaching the solar spectrum(6,8). Power generated light bulb hologen lamp on average, which is 9,9 W/m² measured using a solar power meter SM206. 
[image: image5.jpg]



Figure 1. Sun simulator using hologen bulb lamp.
Figure 2 shows the thermal oxidation results of the Cu plate. The Cu2O layer is more dominantly formed by thermal oxidation for 120 minutes and 100 minutes as compared with 80 minutes. In addition, impurities found in the Cu2O-120 layer as compared with the Cu2O-100.

[image: image6.jpg]



(a)

[image: image7.jpg]



(b)

[image: image8.jpg]



Figure 2. Thermal oxidation of the Cu at a temperature 550 °C for, a) 80 minutes, b) 100 minutes, dan c) 120 minutes.
[image: image9.jpg]I(mA)

180
162

56

vk, Ymal

— Cu/Cu20-80
—— Cu/Cu20-100
—— Cu/Cu20-120

70 84 o8 112 126

V (mV)

140




Figure 3. Characteristic current and voltage of Cu/Cu2O solar cells as a variation of aplied resistor.
Figure 3 shows current plots for all samples as a fuction of voltage. Current on Isc (0 mV) increases when the Cu plate in thermal oxidation for 120 minutes compared with a sample of Cu/Cu2O-80. The current value for Cu/Cu2O-100 samples even higher, ie 1,7 mA. In addition, the overall current value for all samples decreases with increasing voltage. The decrease is a result of the resistor (R) variation given to all samples, ie 0-10 kΩ. Cu/Cu2O-80 samples shows a decrease current at about 10 mV as compared to the Cu/Cu2O-120 which has a decreases at around 45 mV. It is also found that the Cu/Cu2O-100 show greater current values than the Cu/Cu2O-80 and Cu/Cu2O-120 at all voltage. 

Plots Vmak and Imak in Figure 3 determine the Pout value when an optimal resistor (Ropt) is given to a sample of solar cell. As a result, the FF value, which can be determined from the values Pout, Isc, and Voc with respect to variations in resistor values. The FF values for all samples are presented in Table 1. 
The initial analysis in determining the η of the solar cells is Pout value of characteristic I-V. Note that the Cu/Cu2O-80 has Pout value of 0,0031 mW. Table 1 present the Pout values and η solar cells for all the Cu/Cu2O samples. In general, Pout value increases with increasing applied thermal oxidation time. The η solar cells value of the Cu/Cu2O-100 is higher than that of the Cu/Cu2O-120. This show that the Cu2O layer formed on the Cu plate through thermal oxidation affects the diffusion of electrons to the hole in the solar cell. In addition, impurities in Cu plate prevent the formation of Cu2O layer(5).

Table 1. Characteristik I-V and efficiency to the Cu/Cu2O solar cells
	Sample
	Isc
(mA)
	Voc
(mV)
	Imak
(mA)
	Vmak
(mV)
	Pout
(mW)
	FF
	η

(%)

	Cu/Cu2O-80
Cu/Cu2O-100
Cu/Cu2O-120
	0,40
1,70

1,30
	27,70
128,60

139,50
	0,20
0,95

1,00
	15,70
73,90

60,80
	0,0031
0,0702

0,0608
	0,28
0,32

0,34
	0,01
0,28

0,25


Conclusion
  Sun simulator can measure current and voltage as characteristic I-V. The Pout value increases as the addition of thermal oxidation time, but not for the Cu/Cu2O-120 sample. The highest value is owned by Cu/Cu2O-100 (i.e. 0,0702 mW) compared Cu/Cu2O-120 (i.e. 0,0608 mW) and the lowest is owned by Cu/Cu2O-80 (i.e. 0,0031 mW). Then these values and FF can be analyzed further value η solar cells. The η solar cells value increased with the addition of thermal oxidation time, i.e. 0,28% for Cu/Cu2O-100 and Cu/Cu2O-120 is 0,25 %.
Acknowledgment 
One of the authors (TA) thankful to the Ministry of Research, Technology and Higher Education, Republic of Indonesia for research. In addition, the authors would also like to thank the LPPM Samudra University to provide finance support through PDM Program No. 451/UN54.6/LT/2018 given to TA.
References
1. 
Setiawan F. Pembuatan Prototype Solar Cell Sederhana Menggunakan Bahan Tembaga dengan Media Air Laut. J Tek STTKD. 23 July 2017; 4(1). 
2. 
Kaur J, Bethge O, Wibowo RA, Bansal N, Bauch M, Hamid R, dkk. All-oxide solar cells based on electrodeposited Cu2O absorber and atomic layer deposited ZnMgO on precious-metal-free electrode. Sol Energy Mater Sol Cells. 1 Maret 2017;161:449–59. 

3. 
Liu L, Xi Q, Gao G, Yang W, Zhou H, Zhao Y, dkk. Cu2O particles mediated growth of perovskite for high efficient hole-transporting-layer free solar cells in ambient conditions. Sol Energy Mater Sol Cells. 1 December 2016; 157:937–42. 

4. 
Uranus H. Fabrikasi dan Karakterisasi Solar Cell Oksida Tembaga yang Dibuat dengan Teknologi Sederhana. J Elektro. 1 April 2017;10:53–62. 

5. 
Lee S-K, Hsu H-C, Tuan W-H, Lee S-K, Hsu H-C, Tuan W-H. Oxidation Behavior of Copper at a Temperature below 300 °C and the Methodology for Passivation. Mater Res. Februari 2016;19(1):51–6. 

6. 
Soni P. Fabrikasi Sel Surya Berbasis A-Si:H Lapisan Intrinsik Ganda (P-Ix-Iy-N) Dengan Pecvd Dan Analisis Efisiensinya. Institut Teknologi Sepuluh Nopember; 2017.
7. 
Karki IB. Effect of Temperature on the I-V Characteristics of a Polycrystalline Solar Cell. J Nepal Phys Soc. 28 Januari 2016;3(1):35–40. 

8. 
Martil I, Diaz GG. Determination of the dark and illuminated characteristic parameters of a solar cell from I-V characteristics. Eur J Phys. 1992;13(4):193. 

*Corresponding author.

   E-Mail: andifadly@unsam.ac.id

